SUPPLY OF SILICONE OIL - 2013-14

| Specification | QUANTITY IN KG |  |  |
| --- | --- | --- | --- |
|  | Peroorkada factory, Thiruvananthapuram | Kanakala Factory, Belgaum | CSEZ, Kakanadu, Kochi |
| (i) Grade : Matching USP/BP/EP Grade (ii) Chemical Name : Poly Dimethyl Siloxane (iii) Characteristics : Clear, colourless, odourless liquid (iv) Acidity : Not more than 0.10ml. of 0.050N Alcoholic Potassium Hydroxide (v) Identification : Matches standard spectra (vi) Viscocity (at 250C) : 332.5 to 367.5 CST (v) Loss on heating (at 1500C for 2hrs) : 0.3% max. (vi) Specific gravity (at 250C) : 0.965 to 0.973 (vii) Refractive Index at 250C : 1.4013 to 1.4053 (viii) Phenylated compounds : 0.2max (ix) Heavy metals : 5ppm max (x) Assay IR (%) : 97-103 % (xi) Toxicity : Non toxic/Nonirritant to human skin (xii) Packing mode : In Totes of 950kg or 200kg Drums (xiii) The product being offered should have a minimum shelf life of 6 years. (xiv) The supplier has to submit the report of cytotoxicity, skin irritation, skin sensitization, acute systemic toxicity and acute oral toxicity from labs having National or International accreditation at a frequency of once in a year. | 4,50,000 | 85,000 | 75,000 |