SUPPLY OF CENTRIFUGED LATEX 2013-14

| Specification | QUANTITY IN KG |  |  |
| --- | --- | --- | --- |
|  | Peroorkada factory, Thiruvananthapuram | Kanakala Factory, Belgaum | Gajwel Factory, Medak |
| 1. Appearance : Clear milky white colour without grey/yellow 2. Odour : No putrefactive odour after the neutralization of Ammonia with Boric Acid. 3. DRC (%) : 60.0 min. by wt. 4. TS - DRC (%) (NRC) : 1.0 Max. 5. Total Alkalinity (%) (Titration method) : 1.8 - 2.5 6. Viscosity (B -Type Viscometer at 25ºC & 60% TS) (CP) : 50 – 85 7. VFA No. (KOH g/100g Solid) : 0.05 Max. 8. MST (Second) : 800 – 1200 9. KOH No. : 0.6 Max. 10. PH Value at 25ºC : 10 –11.5 11. ZOV (Viscosity after adding 5g. of 40% ZnO) after 5 minutes & to original Viscosity : A Maximum of 25% thickening compared at 25ºC (CP) 12. ZOV after 60 minutes & at 25ºC : A maximum of 30% thickening (CP) compared to original Viscosity. 13. ZST after 60 minutes (Sec.) : 75 (min) or at least 9% retention of the original MST. 14. ZHST after 60 minutes (Sec.) : 200 – 450 at 90 ± 2ºC | 40,00,000 | 6,20,000 | 5,00,000 |